Condiciones de crecimiento de InGaN cúbico

Tabla extraída solo del borrador del artículo.

Título. Growth-controlled carrier redistribution and negative thermal quenching in cubic InGaN/GaN quantum wells on 3C-SiC(001)/Si

Fragmento de crecimiento

The structures were grown by migration-enhanced epitaxy under continuous active nitrogen. The three quantum wells were deposited with a common sequence but at different temperatures, whereas the GaN barriers were grown at 720 °C. MME914 represents the high-temperature limit, with well temperatures of 470–490 °C and short 2 s Ga-on/2 s Ga-off barrier cycles. MME925, MME930 and MME931 used 30 s Ga-on/30 s Ga-off barriers. Their well temperatures decreased progressively, reaching 427 °C in MME925, 417/410/400 °C in MME930 and 400/390/380 °C in MME931. The N2 flow (0.30 sccm in MME914, 0.26 sccm in MME925 and MME930, 0.28 sccm in MME931) was adjusted so that the MBE pressure was 4.2×10−6 Torr in every growth.

| Muestra | Temperatura de los pozos (°C) | Barreras de GaN (°C) | Ciclo Ga-on / Ga-off | Flujo de N₂ (sccm) | Presión MBE (Torr) |
| --- | --- | --- | --- | --- | --- |
| MME914 | 470–490 (intervalo; no hay un valor por pozo) | 720 | 2 s / 2 s | 0.30 | 4.2×10⁻⁶ |
| MME925 | 427 (un solo valor) | 720 | 30 s / 30 s | 0.26 | 4.2×10⁻⁶ |
| MME930 | 417 / 410 / 400 | 720 | 30 s / 30 s | 0.26 | 4.2×10⁻⁶ |
| MME931 | 400 / 390 / 380 | 720 | 30 s / 30 s | 0.28 | 4.2×10⁻⁶ |